Nozzle Component Failure (continued)

Figure 5-4

Figure 5-5

Corrosive abrasion of the pintle nozzle edge

caused by direct contact with blow-by of the combustion gases in the combustion chamber. (Figure 5-4)

Nozzle seat damage caused by metal

contaminants in the fuel that pressed onto the seat area.	The condition can cause leaks or

distorted spray patterns from improper nozzle

seating. (Figure 5-5)

Pintle valve abrasion caused by sulfuric acid.

This condition will cause the nozzle to stop functioning. (Figure 5-6)

Figure 5-6

46