Us&d Oil Sample Data (Limits)

Item	Unit of Measurement.	Limit

Kinematic Viscosity	(@ 98.g°C (CST)/210°F	-20 to 50% ofnewoil

I

1 Total Base No.	I KOH mG/G	I 1 (min.)

Total Acid No.	KOH mG/G

B-Heptane Insoluble	Wt%

Resin Insoluble	wt% Ash Sulfate	wt%

3 (max.)

3 (max.)

Reference [ 1 (max.)] Reference [0.5 (max.)]

1 Diesel Fuel Content

IWt%

I 5 (max.)

I Water Content

lwt%	I .5 (max.)	I

Worn Metal particle: Fe

PPM

150

I Worn Metal particle: Cu	I PPM	I50	I

Worn Metal particle: PB

Worn Metal particle: Cr

PPM

PPM

50

‘20 (or 80..Cr=plated liner)

Worn Metal particle: Al

Worn Metal particle: Si

PPM	20-40

PPM	20

Based on testing a new oil sample of exact same kind as used oil.

57